## Slide 1
SPECTRAL PROPERTIES, AGGREGATION BEHAVIOR IN SOLUTIONS AND
NANOSTRUCTURED DELIVERY SYSTEMS OF
BORON(III)DIPYRROMETHENE LUMINOPHORS
Antina L.A., Kalinkina V.A., Kalyagin A.A., Berezin M.B., Antina E.V.
Conference cluster 2021
Antina L.A. et.al.

## Slide 2
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Excellent photophysical properties of BODIPYs:
BF2-dipyrromethene complexes
strong absorption and fluorescence throughout the UV–vis region which could be tuned towards the near-IR region;
high photochemical and thermal stability;
high molar extinction coefficient and fluorescence quantum yield;
ease synthetic functionalization;
tunable electronic and photonic properties;
low cytotoxicity and good biocompatibility.

## Slide 3
APPLICATION POSSIBILITIES OF BODIPYs:
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
OPTICAL DEVICES
BIOMEDICAL
photodynamic therapy
luminescence bioimaging
laser dyes
organic light-emitting diodes (OLEDs)
fluorescent sensors
biological labeling
electron-transporting materials (ETMs)
drug delivery agents

## Slide 4
Practical use limitations of BODIPYs:
Aggregation caused emission quenching (ACQ) effect ;
strong intermolecular interactions
(π-π stacking) induced by planar π-conjugated structures
Self-absorption induced by small Stokes shift;
High hydrophobicity.
weak fluorescence
of BODIPYs in the
solid-state
and water-organic
systems
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Problems !!!
H-aggregate
J-aggregate

## Slide 5
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
BODIPY PROBLEM SOLVING STRATEGIES
Construction of efficient fluorescent BODIPYs aggregates
HOW DOING THIS???
BODIPY structure design
Metal-organic frameworks (MOFs);
AIE-type molecules
Environment nature
1
2
Use of nanoscale BODIPY carriers:
Changе environmental conditions
WHAT KIND???
Metal-organic cages (MOCs);
Micelles;
Сarbon nanoparticles;
Polymer capsules;
Water-soluble molecules
Temperature, pH…

## Slide 6
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
BODIPY structural modification
5
2
3
4
1
6
7
8
meso position
β positions
α position
β positions
α position
two main directions
introduction of bulky aryl substituents
introduction of extended aliphatic alkyl substituents
into the ms-spacer and
α, β -positions of pyrrole nuclei
Rmeso
https://doi.org/10.3389/fchem.2019.00712
doi:10.1016/j.apsusc.2017.04.014
http://dx.doi.org/10.1007%2Fs00706-019-02521-4

## Slide 7
Objects
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
meso; meso/α subtitution
β subtitution
BDP1
BDP2
BDP3
BDP8
BDP5
BDP4
BDP6
BDP7
"luminophore structure → conditions → properties of supramolecular structures"
Aggregation behavior of BODIPYs in water-organic mixtures / mono- and multilayer Langmuir-Schaefer (LS) films

## Slide 8
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
monomer
aggregates
Daylight
UV light
CBDP1, μM
Absorption
Emission
The absorption and emission spectra of BDP1 in TGF-water mixture (fw=97,5%) at different concentrations of BDP1
Aggregation behavior of BDP1 and BDP5 in water-organic mixtures
CBDP1, μM
The absorption and emission spectra of BDP5 in ACN-water mixtures
H-aggregation
BDP1
BDP5

## Slide 9
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Aggregation behavior of BDP2 – BDP4 in water-organic mixters
The absorption BDP2 in ACN-water mixture (fw=97,5%) at different concentrations BDP2.
CBDP2, μM
The emission spectra of BDP2 in ACN-water mixture (fw=97,5%) at different concentrations of BDP2.
The absorption spectra of BDP4 in TGF-water mixture (fw=97,5%) at different concentrations of BDP3
The absorption and emission spectra of BDP4 in TGF-water mixtures (CBDP3=6.5 μM) with varied volumetric fractions of water (fw)
J-aggregation
H- and J-aggregation
The fluorescent micrographs of LS- and drop-casted films of BDPs, filter with λex = 410–490 nm (n is the touchdowns number)
BDP2
BDP3
BDP2
BDP4

## Slide 10
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Aggregation behavior of BDP6-BDP8
UV-light, ACN
The absorption and emission spectra of BDP6 in ACN-water mixtures (CBDP6=6.5 μM) with varied volumetric fractions of water (fw)
Visible light, 98.5% H2O
The absorption and emission spectra of BDP6 in ACN-water mixtures
(fw = 97.5%) at different concentrations of BDP6
ACN
H2O
50 mkM BDP6
UV light
ACN
H2O
50 mkM BDP6
Visible light
H- and J-aggregation
UV light
fW=0%
fW=97.5%
Drop-cast
The absorption and emission spectra of BDP7 in TGF-water mixtures (CBDP7=6.5 μM) with varied volumetric fractions of water (fw)
The absorption spectra of BDP8 in ACN-water mixtures
(fw = 97.5%) at different concentrations of BDP8

## Slide 11
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
The influence of BODIPYs structure design on aggregation behavior of BODIPYs
meso subtitution
β subtitution
meso/α subtitution
H-aggregation
J-aggregation
H- + J- aggregation
H- + J- aggregation

## Slide 12
Pluronic micelles for BODIPYs solubilization
Pluronic block copolymer molecule
Micelle with a solubilized dye
Bistyryl-BDP
Hal-BDP
Monostyryl-BDP
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Bistyryl-ОН BDP
BDP conjugates with terpenoids

## Slide 13
Preparation of BDP4 - loaded Pluronic® F127 micelles
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Bistyryl-BDP
thin-film method
Control of aggregation and increasing the solubility of distyryl-BDP in aqueous media
Nature of the initial organic solvent.
Solubilization efficiency. Increase in Pluronic® concentration at constant dye concentration
Solubilization capacity. Increasing BDP сoncentration at сonstant Pluronic® сoncentration
Ambient conditions: temperature, nature of the buffer solution, pH, etc.

## Slide 14
Pluronic micelles for BODIPYs solubilization
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Absorption and fluorescence spectra of distyryl-BDP (CBDP4 = 7·10-6 mol/L) in water at different Pluronic® concentrations (λex = 600 nm, gap 5) and the dependences of the absorbance and fluorescence intensity of distyryl-BDP on the content of Pluronic® F127 in water.
τBPD4–Pl (Н2О) = 2.07 ns;
τBPD4–Pl (PBS) = 2.15 ns;
τBPD4-Pl (THF) = 2.41 ns.
QYBPD4–Pl (Н2О) = 19%;
QYBPD4–Pl (PBS) = 20%;
QYBPD4 (THF) = 22%
The dependence of the fluorescence quantum yield and the fluorescence lifetime of BDP4 vs. the organic solvent nature

## Slide 15
Pluronic micelles for BODIPYs solubilization
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
Absorption and fluorescence (λex = 600 nm) spectra of BDP6 in water with different dye content (Cdistyryl-BDP = 7·10-6 ÷ to 5.25·10-5 mol/L) and a constant concentration of Pluronic® (СPl = 3.5·10-4 mol/L), (λex = 600 nm, gap 2)
The dependences of the average diameter of distyryl-BDP–Pl micelles on different concentrations of distyryl-BDP at constant Pluronic® (CPl = 3.5·10-4 mol/L) concentration in water.
Photo of solutions of BPD4-loaded Pl micelles in water at a constant content of Pluronic® (СPl = 3.5·10-4) and an increase in the content of the dye.
Photo of solutions of BDP conjugates with terpenoids loaded Pl micelles in water at a constant content of the dye and an increase in the content of Pluronic®

## Slide 16
3D-architectures based on metal-organic frameworks (MOFs) for the point delivery of BODIPYs
MOF – BODIPY
Zif8 - BODIPY
G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Russia
One-Step synthesis of nanoscale zeolitic imidazolate frameworks with BODIPY loading
SEM image of BODIPY@Zif8 NPs
obtained under different synthesis conditions
MOF – bis(BODIPY)
Autodock 4.2

## Slide 17
Спасибо за внимание