## Slide 2
TRIBENZO-1,4-DIAZEPINOPORPHYRAZINES AS PERSPECTIVE PHOTOSENSITIZERS WITH BREAKDOWN OF THE KASHA-VAVILOV’S RULE
P.A. Tarakanov,1,2 A.O. Simakov, M.E. Neganova,1 D.V. Mischenko,2,3 S.D. Bondarenko,2,4 P.A. Mikhina,2,4 I.A. Sergeeva,4 K.V. Fedorova,4 A.R. Krot,4 N.S. Goryachev,2,4 M.S. Kukharsky,1 S.A. Pukhov,1 V.E. Pushkarev1
1Institute of Physiologically Active Compounds RAS, 142432 Chernogolovka, Russia
2Institute of Problems of Chemical Physics RAS, 142432 Chernogolovka, Russia
3 Research and Education Center of Moscow State Regional University in Chernogolovka, Mytishchi, Russia
4 M.V. Lomonosov Moscow State University, 119991 Moscow, Russia

## Slide 3
Molecular
structure
Photophysical properties
Photochemical properties
Study in cell
cultures
Nano-construction of
PSs in water solutions
Animal model
Interaction with tissue homogenate
Interaction with blood serum
Path to preclinical studies

## Slide 4
Synthesis
Macroheterocycles 2018 11(3) 312-315

## Slide 5
Particular structural features of 6-substituted 5,7-bis(2’-arylethenyl)-6H-1,4- diazepine-2,3-dicarbonitrile
Org. Biomol. Chem., 2016, 14, 1138-1146; Macroheterocycles 2018 11(3) 312-315

## Slide 6
Ellipsoid style presentation: A, B – top and front view, respectively (hydrogen atoms are omitted for clarity).
Capped sticks style presentation with color by symmetry equivalence, hydrogen bonding and short contacts options were applied: C – top view.
Strong intermolecular hydrogen bonding interactions in 1,4-diazepineporphyrazines
Dalton Trans., 2018, 47, 14169-14173

## Slide 7
The extent of dimerization could be modulated by the specific choice of peripheral diazepine substituents
Dalton Trans., 2018, 47, 14169-14173; J. Porphyrins Phthalocyanines 2021, 25, 1204-1211
The spectral changes resulting from changes in the peripheral substituents and solvent conditions. Py = pyridine. CM = 2–5 μM. CM(TBAF) = 500 μM.

## Slide 8
The extent of aggregation could be modulated by the specific choice of peripheral diazepine substituents
Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy 139 (2015), 464–470

## Slide 9
4a/DAPI
4b/DAPI
4a
4b
complexes | FF
 | lexcited = 620 nm
4a | 0.35 ±0.04
4b | 0.05 ±0.005
The fluorescence quantum yields of 4a,b
Time dependence of degree of dissociation of 4a,b in rat brain homogenate (RBH) obtained by fluorescence measurements (C= 10 mM)
Fluorescence image of MCF-7 cells with micellar forms of 4a,b 10 mM
The extent of aggregation of PSs in MCF-7 cells and rat brain homogenates

## Slide 10
Photophysical and Photochemical properties
complexes | FF |  | ФD | 
 | Excited |  | Excited | 
 | Qx | Qy | Qx | Qy
4a | 0.5 ±0.05 | 0.35 ±0.04 | 0.34 ±0.03 | 0.62 ±0.06
Table 1. The fluorescence and singlet oxigen quantum yields of 4a depend on the excitation wavelength
Normalized absorbance and fluorescence spectra of 4a

## Slide 11
TD DFT calculations and natural transition orbital analysis
HOMO
HOMO-1
HOMO-3
LUMO
LUMO+1
LUMO+2
S1x: E=2.110 eV
H-3 -> L+1 (0.08)
H -> L (0.85)
S1y: E=2.255 eV
H-3 -> L (0.10)
H-1 -> L (0.05)
H -> L+1 (0.79)
T1x: E=1.044 eV
H -> L (0.91)
H -> L+2 (0.05)
T1y: E=1.178 eV
H -> L+1 (0.95)
T2: E=1.825 eV
H-1 -> L (0.60)
H-1 -> L+2 (0.24)
Fermi golden rule:
DE: (S1x-T2) = 0.29 eV; (S1y-T2) = 0.43 eV; (S1x-T1y) = 0.93 eV
Charge transfer SOC
The mechanism responsible for triplet generation in these system (S (pp*) → T (CT*)) is similar to the ISC involving S (pp*) → T (np*) transitions and hence greatly enhancing the ISC (El-Sayed’s rule). 1y-2kISC > 1y-xkIC that lead to anti-Kasha effect.
S2: E=2.702 eV
H-1 -> L (0.80)
H-1 -> L+2 (0.04)

## Slide 12
Nano-construction of PSs in water solutions
4b
5b
The micellar forms of PSs based on polyvinylpyrrolidone (PVP) contain 3-4% of complexes.
4a
The liposomal forms of PSs based on lecithin from egg yolk contain 1% of complexes.

## Slide 13
Dynamic light scattering of nano-construction of PSs in water solutions
Comparison of the micellar solutions samples of 4b-PVP size distributions obtained by processing correlation functions in the DynaLS program.
4b
Intensity Distrib (nm)
1e+6
1e+4
100
1
1e+8
Sample | Average hydrodynamic radius of the component, nm | Average contribution of component intensity*, %
4a-PVP | 56 ± 12 | 25
4b-PVP | 50 — 450 | —
5b-PVP | 46 ± 9; 2.5 ± 0.8 | 42; 18
Table 2. Hydrodynamic radius of nanoparticles in micellar forms of complexes
Dependence of the hydrodynamic radius Rh 4a-PVP, 5b-PVP on the concentration of complexes in an aqueous solution.
Chart: 
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
R2, нм | 32.04 | 31.77 | 32.73 | 33.69 | 34.66 | 36.16 | 38.83 | 35.44 | 33.84 | 38.75 | 42.77 | 43.02 | 42.52 | 41.36 | 42.87 | 48.89 | 56.08 | 58.67 | 55.85 | 54.16
R1, нм
1.2
0.8
0.4
0
С, mM
1.6
2
Rh, nm
20
40
60
80
Chart: 
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100
R2, нм | 32.48 | 34.73 | 37.42 | 31.51 | 38.34 | 38.01 | 38.7 | 37.18 | 37.18 | 37.18 | 43.26 | 43.26 | 43.26 | 48.28 | 49.9 | 48.75 | 45.63 | 43.26 | 43.41 | 45.67
R1, нм | 3.74 | 2.1 | 2.045 | 2.1 | 2.72
1.2
0.8
0.4
0
С, mM
1.6
2
Rh, nm
10
30
50
70
4a-PVP
5b-PVP

## Slide 14
Time dependence of degree of dissociation of the complexes in fetal bovine serum (FBS) obtained by fluorescence measurements (C= 10 mM)
Time dependence of degree of dissociation of complexes in rat brain homogenate (RBH) obtained by fluorescence measurements (C= 10 mM)
Interaction with blood serum and with tissue homogenate
Membranes
Proteins

## Slide 15
The extent of aggregation of PSs in MCF-7 cells
Fluorescence image of MCF-7 cells with micellar forms of complexes10 mM (A- 4a, B- 4b, C- 5b)
The fluorescence quantum yields and average hydrodynamic radius (Rh) of the complexes
complexes | ФF (Qy) | Rh, nm
4a | 0.35 ±0.04 | 56 ± 12
4b | 0.05 ±0.005 | 50 — 450
5b | 0.03 ±0.003 | 46 ± 9; 2.5 ± 0.8
Relative integrated density of fluorescence intensity of complexes in cells
Degree of dissociation of complexes in rat brain homogenate (RBH)

## Slide 16
complexes | ФD (Qy) | ФF (Qy) | Rh, nm
4a | 0.62 ±0.06 | 0.35 ±0.04 | 56 ± 12
4b | 0.35 ±0.04 | 0.05 ±0.005 | 50 — 450
5b | 0.35 ±0.04 | 0.03 ±0.003 | 46 ± 9; 2.5 ± 0.8
Table 3. The singlet oxigen quantum yields and average hydrodynamic radius (Rh) of the complexes
Photoinduced cytotoxicity of complexes (1 mM) toward MCF-7 cells using 4 J/cm2 dose light (670 nm, LED).
In vitro analysis of photodynamic activity using MCF-7 cells and rat brain homogenates
Degree of dissociation of complexes in rat brain homogenate (RBH)
Relative integrated density of fluorescence intensity of complexes in cells

## Slide 17
Conclusions
The simultaneous presence of substituents at the C5, C6, and C7 positions of the 1,4- diazepine heterocycle results in effective intramolecular steric interactions, which, in turn, significantly affect the temperature dependent stability of the conformational state of the molecule. It can provide ways of controlling the selective synthesis of low-symmetry A3B-type 5,7-arylethenyl substituted-6H-1,4-tribenzodiazepinoporphyrazines based on temperature dependent steric effect in 5,6,7-substituted-1,4-diazepine-2,3-dicarbonitrile during cross-condensation under Linstead macrocyclization conditions.
The presence of conformation lability and ability of 1,4-diazepine moiety to form intermolecular hydrogen bonding provides control of the tendency of 5,7-arylethenyl substituted-6H-1,4-tribenzodiazepinoporphyrazines to aggregate in different mediums.
1,4-Diazepine moiety in tribenzodiazepinoporphyrazines has strong effect on the decay paths of the excited state based on spin–orbit charge-transfer ISC (SOCT-ISC), which results in anti-Kasha effect.
In vitro study showed possibility to create nanoscale heavy-atom-free photosensitizers with drug release effect based on low-symmetry A3B-type 5,7-arylethenyl substituted-6H-1,4-tribenzodiazepinoporphyrazines in PVP polymer matrix.
1
2
3
4

## Slide 18
Спасибо за внимание
Тетрапиррольные макроциклы как перспективная основа для создания тераностиков
Acknowledgements. The work was financially supported by the RSF (Grant 17-73-10413).
Лаборатория фталоцианинов и их аналогов ИФАВ РАН, Черноголовка, Россия
Лаборатория биохимии патологических процессов ИФАВ РАН, Черноголовка, Россия
Группа экспериментальной химиотерапии опухолей ИПХФ РАН, Черноголовка, Россия
Лаборатория молекулярной биологии ИПХФ РАН, Черноголовка, Россия
Лаборатория химической физики ферментов ИПХФ РАН, Черноголовка, Россия
Лаборатория генетического моделирования нейродегенеративных процессов ИФАВ РАН, Черноголовка, Россия
Лаборатория природных соединений ИФАВ РАН, Черноголовка, Россия
МГУ имени М.В. Ломоносова, физический факультет, отделение экспериментальной и теоретической физики, кафедра молекулярных процессов и экстремальных состояний вещества, Москва, Россия
Группа синтеза порфиразинов НИИ макрогетероциклов (ИГХТУ), Иваново, Россия