## Slide 1
Lomonosov Moscow State University, Department of chemistry
Tatiana Dubinina
Mono and binuclear porphyrazines with annelated
carbazole units:
synthesis and optical properties
XIV International conference "Synthesis and application of porphyrins and their analogues"

## Slide 2
Heteroannelated porphyrazines
Kimura M, Suzuki H, Tohata Y, Ikeuchi T, Yamamoto S, Kobayashi N. Asian Journal of Organic Chemistry 2017; 6: 544-50

## Slide 3
Drugs containing carbazoles
Synthetic materials for LEDs
containing the carbazole moiety
Advances in Heterocyclic Chemistry, eds. E. F. V. Scriven and C. A. Ramsden, Academic Press, 2019, vol. 129, pp. 1-88
antibiotics

## Slide 4
Carbazole unit as a functional group in phthalocyanines

## Slide 5
Example of binuclear phthalocyanine with carbazole linker
Dyes and Pigments 2003, 58, 135–143

## Slide 6
The main objects of study
mononuclear carbazole-fused porphyrazines
Binuclear porphyrazines with carbazole linker

## Slide 7
Synthesis of mononuclear carbazole-fused porphyrazines
Conditions of cross-coupling stage | Result
[Pd(PPh3)2]Cl2, 1,4-dioxane, K2CO3(sat.), Δ | low conversion
Pd(PPh3)4, 1,4-dioxane, K2CO3(sat.), Δ | low conversion
Pd(PPh3)4, toluene, EtOH, K2CO3(sat.), 2M, Δ | low conversion, phthalocyanine admixture
Pd(dppf)Cl2, toluene, EtOH, K2CO3(sat.), 2M, Δ | phthalocyanine admixture
Pd(dppf)Cl2, 1,4-dioxane, K2CO3(sat.), Δ | complete conversion

## Slide 8
Synthesis of mononuclear carbazole-fused porphyrazines
Only one of potential isomers is shown

## Slide 9
Identification of carbazole-fused porphyrazines
1H NMR spectrum of Mg complex 4 measured in [D7]DMF
MALDI TOF (positive ion mode) of Mg complex 4, isotopic pattern (inset A) and simulated MS pattern (inset B)

## Slide 10
UV-Vis spectra of zinc carbazolocyanine and unsubstituted zinc phthalocyanine in DMF
UV-Vis spectra of magnesium carbazolocyanine (4) and corresponding ligand (6) in DMF
UV-Vis spectroscopy of carbazole-fused porphyrazines

## Slide 11
Binuclear porphyrazines with carbazole linker

## Slide 12
Chem. Commun., 2012, 48, 4365
Inorg. Chem. Front., 2017, 4, 110
Dyes and Pigments, 2014, 9, 163
Dyes and Pigments, 2012, 93, 1471
Extension of π-system

## Slide 13
Synthesis of binuclear porphyrazines with carbazole linker: preparation of carbazole linker

## Slide 14
Oxidizing agent | Conditions | Products |  | 
Chloranil | Mesitylene / Δ | + | + | +
DDQ | 1,4-dioxane / Δ | - | + | +
DDQ | о-DCB / 100°C | - | + | +
DDQ | о-DCB / Δ | - | - | +
The most challenging step - oxidative aromatization

## Slide 15
Molecular structure of tetracyano-carbazole

## Slide 16
Synthesis of binuclear porphyrazines with carbazole linker: mixed (statistical) cyclization
Binuclear compound
A3B
A4
A3B
A4

## Slide 17
Synthesis of binuclear porphyrazines with carbazole linker:
direct cyclization

## Slide 18
UV-Vis-NIR and MCD data for tert-butyl-substituted complexes
We thank professor N.Kobayashi for MCD measurements

## Slide 19
835nm
789nm
784nm
712nm
Q band’s positions for planar binuclear complexes
Russian Chemical Bulletin 2006; 55: 1155-58
Inorganica Chimica Acta 2010; 363: 1869-78
Chemical Communications 2012; 48: 4365-67

## Slide 20
Synthesis of binuclear porphyrazines with carbazole linker
UV-Vis-NIR spectra in DMF

## Slide 21
Compound | FD (DMF)
tBu binuclear | 0,15
Ph binuclear | 0,08
PhO binuclear | 0,09
Photosens® | 0,19
lmax = 675 nm
Singlet oxygen quantum yields

## Slide 22
Photodegradation of binuclear porphyrazines
with carbazole linker
degradation
Degradation rate in different solvents:
ν(DMF) > ν(C6H6) > ν(THF)

## Slide 24
Conclusions
Effective synthetic approaches to carbazolocyanines and initial dinitrile were developed
Novel type of planar binuclear porphyrazines sharing a common aromatic bridge were obtained
Photochemical properties, including photodegradation process, were investigated for binuclear complexes

## Slide 25
financial support from
Russian Science Foundation Grant № 21-73-00162
Thank you for your attention!
PhD M.A. Gradova (Semenov Institute of
Chemical Physics),
Prof. N. Kobayashi (Shinshu University)
Group of phthalocyanines and their analogs (MSU):
PhD A.D. Kosov and E.A. Gorbunova
M.Sc. E.O.Moiseeva
students M.S.Belousov, A.S. Agranat, N.E. Kononenko and A.A. Petukhova

## Slide 26
to the memory of Professor Larisa Tomilova (11/04/1947 - 04/01/2021)